## Slide 1: Behavior of material Chapter 6
Doan Manh Hung
Oct 10th, 2014
SCHOOL OF MECHANICAL AND AEROSPACE ENGINEERING

## Slide 2: Chapter 6: Diffusion Mechanism
What are the two atomic mechanisms of diffusion?
How to distinguish between steady-state and non steady-state?
Fick’s first and second law equation form.
Factor that Influence Diffusion.
Diffusion in Ionic and Polymeric Material.

## Slide 3: Diffusion
Phenomenon of material transport by atomic motion.
A diffusion couple, is formed by joining bars of two different metal together so that there is intimate contact between the two faces.
Impurity diffusion or inter-diffusion.
Self-diffusion.

## Slide 4: A copper-nickel diffusion couple

## Slide 5: Diffusion Mechanism
Two condition:
There must be empty adjacent site.
The atom must have sufficient energy to break bonds with its neighbor atom and then cause some lattice distortion during the displacement.
Metallic diffusion:
Vacancy Diffusion
Interstitial Diffusion

## Slide 6: Vacancy Diffusion and Interstitial Diffusion

## Slide 7: Diffusion flux
- Diffusion flux: how fast diffusion occur, or the rate of mass transfer.
Where:
M: mass.
A: area across.
t: diffusion time.
Unit: kg/ or atoms/

## Slide 8: Steady-State Diffusion
Steady-State diffusion:
exist when the diffusion flux dose not change with time.
Concentration gradient =
Concentration gradient =
(kg/)

## Slide 9: Fick’s first law
Diffusion flux for steady-state diffusion (in one direction):
Where: - D diffusion coefficient ()
Fick’s first law driving force => in above equation: the concentration gradient is driving force.

## Slide 10: Example 1

## Slide 11: Non Steady-State Diffusion
The diffusion flux and the concentration gradient at some particular point in a solid vary with time, with a net accumulation or depletion of the diffusing species resulting.
Fick’s first law is no longer convenient => Fick’s second law

## Slide 12: Fick’s second law
The solution are possible when physically meaningful boundary conditions are specified.
The B.C:
Apply B.C to equation above, have:
Where: erf(x/2) is Gaussian error function, a partial listing is given next slide table.

## Slide 13: Tabulation of Error Function Values

## Slide 14: Concentration profile for non steady-state diffusion

## Slide 15: Example 2

## Slide 17: Example 3